

**Product Specifications / Technical Data**

Effective: January 2, 2019

|  |  |  |
| --- | --- | --- |
| Composition: | | Phthalate-Free |
| Installation | | Unilin Locking System |
| Size (inches / mm): | | 8.97” x 59.84” (227.8 x 1519.9mm) |
| Gauge: | | 4.0mm+1.0mm AcoustX G-Core Sound Absorbing Backing=5.0mm |
| Wear Layer: | | 20mil (.5mm) |
| Finish: | | Advanced Urethane Coating |
| Edge: | | Painted Bevel |
| Sq.Ft. / Piece: | | 3.72 |
| Sq.Ft. / Carton: | | 18.65 |
| Pieces / Carton: | | 5 |
| Cartons / Pallet: | | 60 (1,119 sq.ft.) |
| Pallets / 20’ Container: | | 21 (23,499 sq.ft.) |
| Weight / Pallet: | | 1,904.4lbs |
| Limited Warranty: | | Lifetime Residential  10 Year Commercial |
| **Testing** | | |
| ASTM F1700 – Product Classification: | | Class III, Type B, Embossed Surface  Meets and exceeds passing requirements | |
| ASTM E648 – Radiant Panel  (Critical Radiant Flux-Fire Rating Flaming Spread): | | Meets and exceeds passing requirements (Class 1) | |
| ASTM D2047 James Machine – Coefficient of Friction (Slip Resistance) | | Meets and exceeds passing requirements | |
| ASTM F925 – Resistance to Chemicals: | | Meets and exceeds passing requirements | |
| ASTM E492 – Impact Sound Insulation Acoustical Testing (IIC) | | 58 IIC – over 6” concrete | |
| ASTM F970 - Static Load Limit: | | Meets and exceeds passing requirements | |
| **Sustainability** | | |
| Recycled Content: | | No |
| ISO 9001 – Quality Management System: | | Meets and exceeds passing requirements |
| ISO 14001 – Environmental Management System: | | Meets and exceeds passing requirements |
| FloorScore® Certified: | | Yes |

[www.acrylxusa.com](http://www.acrylxusa.com)

1-855 3 RASKIN